| SECTION G STRUCTURAL | Product and manufacturer’s details | Ability to be disassembled, reused, recycled, downcycled YY=yes, easily YH= yes, with high work input N=no U=unknown V-varies according to product | Relevant system features | Non-disassembleable / reusable / recyclable alternatives | Issues to consider | Advantages of reusable/ recyclable option | Frequency of use / examples of reuse / recycling |
| --- | --- | --- | --- | --- | --- | --- | --- |
| STRUCTURAL STEEL FRAMING | Main use: building frames Product: steel | Reuse as new – YY Reuse 2nd hand – YY Recycling – YY Downcycle – YY | Steel beams and columns Steel framing bolted can be unbolted and reused | Welded steel sections are more difficult to reuse, but not impossible. These would have to be cut and appropriate plates welded on. | Sizes will limit the possible reuses. Fire protection has to be designed to be easily removed. Details of steel should be marked on steel section | Installation errors can be adjusted with limited disruption. | Use- common Reuse – uncommon Recycling - common Bed Zed reused steel beams and columns from nearby project. |
| TIMBER FRAMING | Product: Laminated timber Main use: wall and roof structures Manufacturer: Glulam | Reuse as new – YH Reuse 2nd hand – YY Recycling – N Downcycle – YY | Joints are bolted and easily dismantled | Welded steel or concrete frames are more difficult to recycle and difficult if not impossible to reuse | Glulam structures are extremely versatile in terms of use and are generally bolted in place making them easy to disassemble Reuse is limited by design constraints and only downcycling is possible |  | Use – common Reuse – seldom |
|  | Product: reclaimed timber beams/ columns Main use: wall and roof structures | Reuse as new – YH Reuse 2nd hand – YY Recycling – N Downcycle – YY | All connections are bolted and easily dismantled | As above | Old timber beams often were fixed with pegs and can be disassembled or if necessary cut beyond the junction points. TRADA can assess the structural quality of old timber beams to allow their reuse | Old timbers are often thought to have character and enhance the aesthetics of a space | Use – common Reuse – common The Geffrye Museum of English Domestic Interiors in East London has made use of reused pitch pine structural beams |
| Timber floor structures | Main use: floors Product: solid timber. Composite beams or similar | Reuse as new – YY Reuse 2nd hand – YY Recycling – N Downcycle – YY | Any type of timber joists can easily be reused if fixed on joist hangers rather than set within the wall construction | By setting the joist within the wall construction, the disassembly of the floor is hampered, but not made impossible. | Treated timber should be worked with care as treatment toxins can become volatile as a result of the working. Treated timber sections can be reused | Floor structures are generally not visible therefore reused material with potential aesthetic flaws is acceptable. There is therefore a potential long term cost benefit of having a material in the building that can be resold at the end of the building’s life. Also any changes to the floor structure are more easily undertaken ( a timber set in the wall structure being more difficult to remove than a joist hanger) | Use – common |