| SECTION S PIPED SUPPLY SYSTEMS | Product and manufacturer’s details | Ability to be disassembled, reused, recycled, downcycled YY=yes, easily YH= yes, with high work input N=no U=unknown V-varies according to product | Relevant system features | Non-disassembleable / reusable / recyclable alternatives | Issues to consider | Advantages of reusable/ recyclable option | Frequency of use / examples of reuse / recycling |
| --- | --- | --- | --- | --- | --- | --- | --- |
| HOT AND COLD WATER | Product: polybutylene plastic pipework Main use: hot and cold water supply Manufacturer: George Fisher www.georgefisher.co.uk | Reuse as new – YY Reuse 2nd hand – YY Recycling – YY Downcycle – YY | Flexible pipes joined by electro-fusion | Copper pipework can be recycled and reused, but the dismantling is more labour intensive |  | The installation time is typically 2% of that of copper. The work process poses less risk to health. The jointing system does involve soldering with a naked flame and therefore the risk of fire on site is reduced. The material is light and therefore easier to carry. | Commonly available |
|  | Product: crosslinked polyethylene barrier pipe Main use: hot and cold water supply Manufacturer: JG Speedfit www.speedfit.co.uk | Reuse as new – YY Reuse 2nd hand – YY Recycling – YY Downcycle – YY | Pushfit system | As previous item. Pushfit are even more easily dismantled than electro-fusion connections | System can be linked to copper system. | As previous item | Commonly available |